## Slide 1: Mobile Asphalt Testing Trailer Program (MATT): Recent Experience in Arizona
Arizona Pavements/Materials Conference November 15, 2018  Tempe, AZ
Office of Preconstruction, Construction, and Pavements
All images FHWA unless otherwise noted.
Amir Golalipour, Ph.D.
David J. Mensching, Ph.D., P.E.

## Slide 2: Agenda
FHWA Pavement and Materials
Binder Activities
Asphalt Mixture Performance Tester (AMPT)
Arizona Project Results & Discussions
Questions

## Slide 3: Acronyms
AASHTO: American Association of State Highway and Transportation Officials
ABCD: Asphalt Binder Cracking Device
ABTL: Asphalt Binder Testing Laboratory
AIMS: Aggregate Imaging System
AMPT: Asphalt Mixture Performance Tester
BBR: Bending Beam Rheometer
CAA: Coarse Aggregate Angularity
CC: Concentric Cylinders
DSR: Dynamic Shear Rheometer
DTT: Direct Tension Tester
ETG: Expert Task Group
Gmb: Bulk Specific Gravity
GTR: Ground tire rubber
HMA: Hot mix asphalt
HQ: Headquarters
MATT: Mobile Asphalt Testing Trailer
MSCR: Multiple Stress Creep and Recovery
PAV: Pressure Aging Vessel
PEMD: Performance-Engineered Mixture Design
PG: Performance Grading
PRS: Performance Related Specification
QA: Quality Assurance
RAP/RAS: Reclaimed Asphalt Pavement/Reclaimed Asphalt Shingles
RTFO: Rolling Thin-film Oven
RV: Rotational Viscometer
SSR: Stress Sweep Rutting
TFHRC: Turner-Fairbank Highway Research Center
WMA: Warm Mix Asphalt
Note: FHWA does not endorse products or manufacturers. Trade or manufacturers’ names appear in this presentation solely for informational purposes.

## Slide 4: Pavement & Materials Discipline
Program Office
  Office of Preconstruction, Construction, and Pavements (FHWA HQ, Washington, DC)
    Mobile Asphalt Testing Trailer (MATT)
    Asphalt Binder Testing Laboratory (ABTL)
Research and Development
  TFHRC (McLean, VA)
Technical Services
  Resource Center
Divisions
Notes: Added R&D, Tech Services, and Divisions

## Slide 5: Program Objective
Provide Support to National Initiatives
  Performance-Engineered Mixture Design (PEMD)
  Increased Pavement Density
  Development of New QA Concepts for HMA
  Understanding Asphalt Rubber Testing
  Binder Performance Testing
Provide Assistance with State-specific Issues
  Technical Guidance
  Forensics

## Slide 6: MATT Program History
Projects began in 1988
  Demonstration Project 74: Field Management of Asphalt Mixes Using Volumetric Quality Control
Transition to Superpave implementation
  Early 1990s
  Classroom and hands-on training
Transition to performance-related specifications
  Shadow testing
  AMPT user since 2003
Innovative materials and practices
  WMA, SMA, GTR, RAP/RAS, increased density

## Slide 7: MATT visits since 2007
Field Work
PR
Workshop/Hands-on Training/Presentation/ Open House/Technical Assistance
Both
Notes: NEW SLIDE

## Slide 8: Technical Workshops

## Slide 9: Training
Training for the Maryland State Highway Administration staff

## Slide 10: Field visits
Notes: NEW SLIDE

## Slide 11: Other MATT Activities
Conferences
Expert task group support
NCHRP panels and project participation
Division Office rotational assignments
Academic journal papers and presentations
Notes: NEW SLIDE

## Slide 12: Deployment Status: Asphalt Rubber
Seven projects between 2013 to 2015
Collaboration with four State DOTs to evaluate their specifications based on project results
Working with FHWA ETG to develop AASHTO standard for asphalt rubber testing

## Slide 13: Binder Activities

## Slide 14: Binder Characterization
TEST PROCEDURES
EQUIPMENT
RV
DSR
RTFO
PAV
Vacuum Degassing Oven
BBR
DTT
ABCD (AASHTO TP 92)
Torsional bar testing
Performance Grading
  AASHTO M 320
  AASHTO M 332 (MSCR)
  AASHTO R 49 (Low Temperature PG)
Solubility & Separation
  AASHTO T 44
  ASTM D7173

## Slide 15: MSCR Criteria: AASHTO M 332 - Jnr
Boundaries for Jnr values are established based upon traffic level.
As traffic level increases, lower Jnr value is required -> basically stiffer binder.

## Slide 16: MSCR Criteria: AASHTO R 92 - R%
% Recovery is plotted vs. Jnr.
Boundaries are established based upon measured Jnr values at 3.2 kPa.
A simple above the line/below the line criteria provides the needed validation of polymer modification.
Good agreement has been established between elastomeric polymer modification and rutting resistance.
% Recovery above the line indicates the binder is modified with an acceptable elastomeric polymer.
% Recovery below the line indicates the binder is not modified with an elastomeric polymer.
Source: Asphalt Institute
Notes: Jnr, or non-recoverable compliance, is simply the unrecovered strain relative to the applied stress.
“Good agreement…” where it come from? What data is there to back this up?

## Slide 17: MSCR Implementation
Source: Asphalt Institute
Notes: NEW SLIDE

## Slide 18: DSR Testing Alternative: Asphalt Rubber Binder
Can it fit within existing PG grading system?
DSR Testing Geometry
  Caltrans, University of California Pavement Research Center, Anton Paar, etc.
  Concentric cylinder (CC) development testing evaluation looks promising.
  CC test geometry may overcome specimen preparation limitations of PP geometry.
  Draft AASHTO standard in development.

## Slide 19: Concentric Cylinder Geometry
Advantages
  GTR modified asphalt can be measured with particle sizes up to 2 mm.
  No trimming problems and filling problems.
  No edge effects.

## Slide 20: Low Temperature BBR Test: Binder New Parameter (∆Tc)
∆Tc has been identified as an important parameter related to asphalt binder durability.
  ∆Tc = S critical temp - m critical temp.
As an asphalt binder ages, ∆Tc value becomes more negative.
  Indicating a loss of relaxation properties.
Threshold of -5 °C being evaluated as a cracking criteria.

## Slide 21: Mixture Activities

## Slide 22: Performance Testing
AASHTO T 378 (former TP 79)
  Dynamic Modulus
    Mixture Stiffness
    Rutting
    Fatigue Cracking
  Flow Number
    Rutting
AASHTO TP 107
  Cyclic Fatigue
AASHTO TP XX
  Stress Sweep Rutting (SSR)

## Slide 23: Small Specimen Testing
Proposed to enable field core testing
To improve the efficiency of laboratory specimen fabrication
Image: North Carolina State University

## Slide 24: Small Specimen Geometry
Need less material to complete testing matrix
Image: North Carolina State University

## Slide 25: Small Specimen Geometry
Imag: North Carolina State University

## Slide 26: Types of Small Specimen Testing
Small Scale Cyclic Fatigue
Small Scale Dynamic Modulus
Notes: 26

## Slide 27: AMPT Small Specimen Advantages
Field core testing
Reduced sampling and material requirements for testing
Same data output generated from small scale testing as full scale testing

## Slide 28: Arizona Project

## Slide 29
Arizona Project Description - 2015
Open Graded Friction Course (OGFC) mixtures
Three different Terminal blended Asphalt Rubbers
Hybrid Binders:
  PG70-22 TR+ (8 % GTR + 2 % SBS; solubility limit of 97%)
  PG70-22 TR+ S92 (8 % GTR + 2 % SBS; solubility limit of 92%)
  PG70-22 (contains only SBS)

## Slide 30
Study Plans
Topics investigated in this project
  Solubility
  Separation
  DSR testing: gap size effect
  Long term conditioning

## Slide 31
Solubility – AASHTO T 44
UW-Madison MARC have proposed changes to the standard
  Use of toluene as the solvent
  The addition of an analytical filter: To increase the filter area and reduce the potential for the fiberglass filter to become clogged during testing
  Analytical Filters used in this study
  Celite
  Diatomaceous Earth (DE)
Notes: DE was included because only 1 to 2 grams of analytical filter aid is needed for each test, and the smallest amount of Celite 505 that can be purchased is a 50 lb. bag, enough for more than 11,000 tests

## Slide 32: Solubility Results
Use of toluene as the solvent
The addition of an analytical filter
Some differences in solubility
Notes: Three amounts of Celite 505 were used: 0.5 g, 1.0 g, and 1.5 g. Based on visual observations, 1.5 g of Celite 505 provided quicker filtration compared to 0.5 and 1.0 g respectively.

## Slide 33: Solubility Results: Analysis of Variance
Compared to Standard Method, AASHTO T 44.
Not a statistically significant difference using toluene compared to trichloroethylene.
The differences in solubility when using an analytical filter aid were 0.5 to 2.5 percent: significant considering solubility is normally specified to the nearest 0.1 percent !
Notes: The lower measured solubility with the analytical filter aid may be due interaction between the filter aid and the modifier that produces agglomerations of modifier that will not pass through the filter.

## Slide 34: Separation Results
Separation tests conducted following ASTM D7173: samples are stored in vertical tubes in an oven at 163 °C for 48 hours
Test specimens taken from the top and bottom of the vertical storage tube are measured using AASHTO T 315
GTR is separating and sinking to the bottom of the separation tube.

## Slide 35: PG Results: PG 70-22 TR+ (S97) 1 & 2 mm gap vs. Cup and Bob
Same PG grade
Cup & Bob (CC 17) slightly higher G*/sinδ value: perhaps due to trimming or shelf-aging of material
Cup & Bob: smallest values of standard deviation
Notes: The true PG grade of PG 70-22 TR+ is PG 75.5 (20.7) -28.8

## Slide 36: PG Results: PG 70-22 TR+ (S92) 1 & 2 mm gap vs. Cup and Bob - Unaged
PP 1mm shows different material behavior
PP 1mm: possible particle interactions with plates -> higher stiffness & more elastic type behavior
Similar results for PP 2mm and Cup & Bob
Notes: The true PG grade of PG 70-22 TR+ (S92) is PG 70-22 TR+ (S 92) -> PG 80.7 (13.1) -32.0

## Slide 37: DSR PG Results: 1 vs. 2 mm gap PG 70-22 TR+ (S 92) – Original binder at 76 °C
For gap sizes of 1 to 2 mm: when there is an interaction of the rubber particles with the testing plates -> ↑ gap : ↓ variability, ↓ the complex modulus, ↑ the phase angle.
Lower G*/sinδ and phase angle for 1mm
Notes: The true PG grade of PG 70-22 TR+ (S92) is PG 70-22 TR+ (S 92) -> PG 80.7 (13.1) -32.0

## Slide 38: PG Results: PG 70-22 TR+ (S92) 1 & 2 mm gap vs. Cup and Bob - RTFO
Same PG grade
PP 1mm: possible particle interactions with plates -> lower phase angle (more elastic type behavior)
Differences decreased after RTFO conditioning
Notes: The true PG grade of PG 70-22 TR+ (S92) is PG 70-22 TR+ (S 92) -> PG 80.7 (13.1) -32.0

## Slide 39: PG Results: PG 70-22 TR+ (S92)
2mm vs. Cup & Bob: most similar results
Differences decreased after RTFO aging …
Notes: The high temperature PG grade of RTFO binder is PG 80.7 (13.1) -32.0 for both 1 mm and 2 mm gap setting.
However, the G*/sinδ and phase angle were higher for 2 mm gap when compared to 1 mm gap.

## Slide 40: DSR PG Results: 1 vs. 2 mm gap Statistical Analysis – Effect of 1mm increase in gap
Only PG 70-22 TR+ (S 92) original binder show effects consistent with particle interaction.
When used to test binders modified with GTR, this gap may be too small to accommodate the rubber particles.
Concentric Cylinder (Cup & Bob) needed as testing geometry for these materials.
Notes: The true PG grade of PG 70-22 TR+ (S92) is PG 70-22 TR+ (S 92) -> PG 80.7 (13.1) -32.0

## Slide 41
Summary of Findings
Solubility: Toluene was found to be an acceptable alternative to Trichloroethylene as a solvent for solubility testing.
Separation: GTR, due to its higher specific gravity than neat asphalt binder, is separating and sinking to the bottom of the separation tube. Separation of TR+ (S 92) binder during non-agitated long-term storage should be expected.
DSR testing: Results indicate that particle interaction with the plates likely occurs when testing the PG 70-22 TR+ (S 92) using the parallel plate geometry.

## Slide 42
Takeaway
Separation: Needs to be considered for Asphalt Rubber Material. (ASTM D7173)
DSR testing: All Asphalt Rubber Binders are not the same ! Some may work with PP and some not. Cup & Bob is a scientific & practical solution.
DSR testing:
  PP issues: trimming, edge effect, particle interactions, rubber swelling, rubber mesh size and percentage, etc.
  Cup & Bob: no trimming, exact volume filling, no edge effect

## Slide 43: Technical Assistance
If you have upcoming projects for which you would like MATT technical assistance, contact:
  Amir Golalipour, amir.golalipour.ctr@dot.gov, 202.366.3982
  Dave Mensching, david.mensching@dot.gov, 202.493.3232
  https://www.fhwa.dot.gov/pavement/asphalt/trailer/
Notes: UPDATED WEBPAGE LINK

## Slide 44: Thank You – Questions?
Trailer is parked outside! Come in for a tour!
We’re here to assist! Please stop by anytime for more discussion.